G-NOR ELECTRONICS CO.,LTD.

| GNL-8003xx (Φ8mm ROUND TYPE) Ultra Brightness ABSOLUTE MAXIMUM RATING:(Ta=25℃) Parameter; Unit. DC Forward Current; 30; mA. Reverse Voltage; 5; V. Reverse Current (Vr-5V); 10; µA. Peak Forward Current ,tw ,=1 msec Duty ,=1/20; 150; mA. Operation Temperature; -40; +80; ℃. Storage Temperature; -40; +100; ℃. Solder Dip (5 seconds,1.6mm from body ) Temperature; 300; ±5; ℃. |  |
| --- | --- |
| Feature: Description: 1.Small flange without stand-off 1.The shape of this series is round 2.Long life-solid state reliability 2.General application is for indication,illumination,etc. 3.Long lead length(25.4mm) 3.These LED lamps are available with a choice of defferent 4.Versatile mounting on P.C. board or panel colors,light intensities,epoxy colors,etc. |  |
| # Part Number; EMITTED COLOR; Lens Color; Peak Wavelength (nm); Vf (v) Typ.; IV (If=20mA) mcd; View Angle 2θ1/2. Min.; Typ.. GNL-8003SRD; GaAlAs; Super Red; Red Diffused; 660; 1.9; 50; 100; 60°. GNL-8003LRD; GaAlAs; Super Red; Red Diffused; 660; 1.9; 200; 400; 60°. GNL-8003SRT; GaAlAs; Super Red; Red Transparent; 660; 1.9; 250; 400; 22°. GNL-8003SRC; GaAlAs; Super Red; Water Clear; 660; 1.9; 250; 400; 22°. GNL-8003LRC; GaAlAs; Super Red; Water Clear; 660; 1.9; 600; 800; 22°. GNL-8003URC; GaAlAs; Super Red; Water Clear; 660; 1.9; 1200; 1500; 22°. GNL-8003UEC; AlGaInP; Super Orange Red; Water Clear; 625; 2.0; 1500; 2000; 22°. GNL-8003HRC; AlGaInP; Super Orange Red; Water Clear; 640; 2.0; 1200; 1800; 22°. GNL-8003UEC-TL; AlGaInP; Super Orange Red; Water Clear; 625; 2.0; 4000; 5000; 22°. GNL-8003UYC; AlGaInP; Super amber; Water Clear; 585; 2.0; 1500; 2000; 22°. GNL-8003UYC-TL; AlGaInP; Super amber; Water Clear; 585; 2.0; 4000; 5000; 22°. GNL-8003UBC; InGaN; Ultra Super Blue; Water Clear; 470; 3.5; 1800; 3500; 22°. GNL-8003UBC-TL; InGaN; Ultra Super Blue; Water Clear; 470; 3.5; 2500; 4500; 22°. GNL-8003UBD-TL; InGaN; Ultra Super Blue; Blue Diffused; 470; 3.5; 1000; 1500; 60°. GNL-8003BC-1; InGaN; Super Blue; Water Clear; 470; 3.5; 1500; 2000; 22°. GNL-8003PGC; InGaN; Super Pure Green; Water Clear; 525; 3.5; 5000; 9000; 22°. GNL-8003PGC-TL; InGaN; Super Pure Green; Water Clear; 525; 3.5; 8000; 12000; 22°. GNL-8003UWC; InGaN; Ultra Super White; Water Clear; 5500K-7000K; 3.5; 4000; 9000; 22°. GNL-8003VC; InGaN; Super Violet; Water Clear; 400; 3.5; 100; 300; 22°. |